Cationic Active Agent DT-222

Product introduction

DT-222 is a special softener of quaternary ammonium salt with amide group. It can give the fabrics soft, fluffy, dry and comfortable hand feelings, and doesn’t affect their hydrophilic property. It is especially suitable for softening the cotton fabrics, cotton blended fabrics, or the kind of fabrics like towel.

Physical and chemical properties

- Appearance	            Pale yellow Paste@20℃；Yellowish Liquid @40℃

- Solid content             ≥88%

- pH（5% in water）        5.0～6.5

- Ion species	             Cationic

- Component              Quaternary ammonium salt with amide group

- Solubility                Soluble in cool and hot water

Product feature

Wide dispersing range（5～20%）

Easy for formulation（Can disperse in cool water）

Good re-wetting property

Both good antistatic and softening property

Preparation

DT-222 can be diluted to any concentration (≤20%) in both cool and hot water when using in applications.

Applications

- DT-222 is suitable for both home and industry water based softener. It is used for lubricating and softening fabrics. The fabrics treated by DT-222 can show well softness and excellent antistatic performance.

- DT-222 used together with silicone oil can give fabrics special hand feelings of soft, smooth and fluffy.

- DT-222 used together with sheet-like softener can substantially improve the hand feelings of fabrics.

- Padding method: Fabrics 10-50g/L (means 10% DT-222 in water) padding for two times→ liquid tack-up 70% → drying

- Dip dyeing method: Fabrics 1-5% (o.w.f)(means 10% DT-222 solution 30～50℃×20～30min) → spin-dry → drying

Package

125kg/drum or 180kg/drum

Storage

Please store at 5-35℃，avoid freezing and exposure to the sun. Its shelf life is 12 months.

The formulations and technology recommended above were based on our knowledge and understanding to our product. Just for reference. We couldn’t ensure that it could be available for all processes, so customers need to test in advance according to specific application conditions.